## Slide 1
Ingredient list |  |  |  |  | 
Element | Fe | C | Mn | Si | Cr
Content (wt%) | Bal. | ≤0.03 | 2.00～3.00 | ≤1.00 | 16.00～18.00
Element | Ni | Nb | S | P | 
Content (wt%) | 10.00～14.00 | 0.15～0.45 | ≤0.03 | ≤0.03 | 
• Other Brands: 022Cr17Ni12Mo2 • Density: 7.9 g/cm3 • Heat Treatment: It is annealed in the temperature range of 850-1050 °C and then rapidly cooled. • Low carbon Austenitic stainless steel, excellent corrosion resistance, good heat resistance, low magnetic after processing.
Mechanical properties |  |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Hardness （HRC） | Tensile strength (σb/MPa）
Content (wt%) | 540 | 450 | 30 | 50 | 28
316L
SLM Physical properties of materials

## Slide 2
Ingredient list |  |  |  |  |  | 
Element | Fe | C | Mn | Si | Cr | Ni
Content (wt%) | Bal. | ≤0.07 | ≤1.00 | ≤1.00 | 15.50 ~ 17.50 | 3.00～5.00
Element | Cu | Nb | S | P |  | 
Content (wt%) | 3.00～5.00 | 0.15～0.45 | ≤0.030 | ≤0.035 |  | 
• Other Brands: 0Cr17Ni4Cu4Nb ， 630 • Density: 7.8 g/cm3 • Martensite precipitation hardening stainless steel, with stable elasticity and high strength, hardness, good welding properties and corrosion resistance. For high strength components with certain corrosion resistance requirements.
Mechanical properties |  |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Section shrinkage （%） | Hardness （HRC）
Content (wt%) | 1300 | 1200 | 12 | 20 | 50
SLM Physical properties of materials
17-4PH

## Slide 3
Ingredient list |  |  |  |  | 
Element | Fe | C | Mn | Si | Cr
Content (wt%) | Bal. | 0.3~0.4 | ≤1.00 | ≤1.00 | 12.00～14.00
Element | Ni | S | P |  | 
Content (wt%) | ≤0.75 | ≤0.03 | ≤0.04 |  | 
• Other Brands: S136 ， • Density: 7.93 g/cm3 • With high wear resistance and corrosion resistance, high hardness, suitable for all kinds of precision machinery, mold, bearings, transportation tools, home appliances, etc. . It is widely used for making parts with resistance to atmosphere, water vapor, water, oxidation and acid corrosion.
Mechanical properties |  |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Section shrinkage （%） | Hardness （HRC）
Content (wt%) | 1050 | 910 | 12 | 30 | 28
420
SLM Physical properties of materials

## Slide 4
Ingredient list |  |  |  |  |  |  | 
Element | Fe | C | Mn | Si | Cr | Ni | Co
Content (wt%) | Bal. | ≤0.03 | ≤0.1 | ≤0.1 | ≤0.5 | 17～19 | 8.5-10
Element | Mo | Ti | Al | Cu | S | P | 
Content (wt%) | 4.5-5.3 | 0.6~0.8 | 0.05~0.15 | ≤0.5 | ≤0.01 | ≤0.01 | 
• Other Brands: 1.2709 ， MS1 • Density: 7.9 g/cm3 • Heat treatment: annealed at 490 ° C for 6 hours, then rapidly cooled。 • Low-carbon Maraging steel are superior in strength, toughness, hardness and abrasion resistance to conventional steel and are used to make components for moulds, automobiles, medical and mechanical industries.
Mechanical properties |  |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Section shrinkage （%） | Hardness （HRC）
Content (wt%) | 1700 | 1650 | 9 | 15 | 36
18Ni300
SLM Physical properties of materials

## Slide 5
Ingredient list |  |  |  |  |  | 
Element | Al | Si | Mg | Fe | Cu | Mn
Content (wt%) | Bal. | 9.0～11.0 | 0.2～0.5 | ≤0.55 | ≤0.05 | ≤0.45
Element | Ni | Zn | Pb | Sn | Ti | 
Content (wt%) | ≤0.05 | ≤0.10 | ≤0.05 | ≤0.05 | ≤0.15 | 
• Other Brands: ZL104 • Density: 2.7 g/cm3 • Heat treatment: annealing at 300 ° C for 2 hours, then air cooling。 • Because of its low density and good corrosion resistance, its castings are widely used in aviation, instrumentation and general machinery, for example, automobile engine cylinder head, intake manifold, piston, wheel hub, steering booster shell.
Mechanical properties |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Hardness （HRC）
Content (wt%) | 280 | 180 | 8 | 120
AlSi10Mg
SLM Physical properties of materials

## Slide 6
Ingredient list |  |  |  |  | 
Element | Ti | Al | V | Fe | C
Content (wt%) | Bal. | 4.0~6..75 | 2.5~4.5 | ≤0.30 | ≤0.10
Element | N | H | O | Other single element | All other single element
Content (wt%) | ≤0.05 | ≤0.015 | ≤0.20 | ≤0.10 | ≤0.40
• Other Brands: TC4 • Density: 4.5 g/cm3 • Heat treatment: annealing at 700 ~ 850 ° C for 2-4 hours, then rapidly cooling。 • The material has small specific gravity, light weight, excellent mechanical properties and corrosion resistance, and is suitable for aerospace and automotive manufacturing fields.
Mechanical properties |  |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Section shrinkage （%） | Hardness （HRC）
Content (wt%) | 895 | 825 | 10 | 12 | 34
Ti6Al4V
SLM Physical properties of materials

## Slide 7
Ingredient list |  |  |  |  | 
Element | Ni | Cr | Nb | Mo | Ti
Content (wt%) | Bal. | 17.0~21.0 | 4.75~5.5 | 2.8~3.3 | 0.65~1.15
Element | Al | Co | Cu | S | P
Content (wt%) | 0.20~0.80 | ≤1.0 | ≤0.30 | ≤0.015 | ≤0.015
• Other Brands: GH4169 • Density: 8.2 g/cm3 • It has high strength and good toughness under 650 ° C and corrosion resistance under high and low temperature.
Mechanical properties |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Hardness （HRC）
Content (wt%) | 1400 | 1100 | 12 | 47
In718
SLM Physical properties of materials

## Slide 8
Ingredient list |  |  |  |  | 
Element | Ni | Cr | Nb | Mo | Fe
Content (wt%) | Bal. | 20.0~23.0 | 3.2~4.2 | 8~10 | ≤5.00
Element | Ti | Al | Co | S | P
Content (wt%) | ≤0.40 | ≤0.40 | ≤1.00 | ≤0.015 | ≤0.015
• Other Brands: GH3625 • Density: 8.4 g/cm3 • The service temperature range is 900 ~ 1300 ° C. it has high high temperature strength, good oxidation and corrosion resistance, good fatigue property, fracture, toughness and other comprehensive properties
Mechanical properties |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Hardness （HRC）
Content (wt%) | 900 | 650 | 30 | 27
In625
SLM Physical properties of materials

## Slide 9
Ingredient list |  |  |  |  |  | 
Element | Ni | Cr | Fe | Al | C | Mn
Content (wt%) | Bal. | 20.5~23.5 | 17.0~20.0 | ≤0.10 | 0.05~0.15 | ≤1.00
Element | Si | Mo | Co | W | S | P
Content (wt%) | ≤1.00 | 8.00~10.00 | 0.5~2.5 | 0.2~1.0 | ≤0.01 | ≤0.015
• Other Brands: GH3536 • Density: 8.3 g/cm3 • High temperature in a variety of atmosphere with corrosion resistance, and has excellent, high-temperature strength, in a variety of high-temperature environment has been widely used.
Mechanical properties |  |  |  | 
Element | Tensile strength (σb/MPa） | Yield (σP0.2/MPa） | Elongation（%） | Hardness （HRC）
Content (wt%) | 650 | 550 | 25 | 24
HX
SLM Physical properties of materials